CHEMICAL, OIL and SOLVENT RESISTANCE

OF POLYURETHANE

Samples of both polyether and polyester

were immersed for seven days at 75

°F.

The rating was

based on volume change according

to

the following *key:

1

=

Excellent

(

0

-

3%)

2

=

Good

(

4

-

15%)

3

=

Fair

(16 - 35%)

4

=

Poor

( 36% Up )

Chemical

Ether

Ester

Acetaldehyde

4

4

Acetic Acid

4-3

Acetic Anhydride

4

4

Acetone

4

4

Acetyl Bromide

3-4

4

Acetyl Chloride

3-4

4

Acetylene

2-3

3

Adipic Acid

1

2

Aluminum Chloride

2

2

Aluminum Sulphate

2

2

Aluminum Sulfide

2

2

Ammonia

2

2-3

Ammonium Acetate

3-4

3-4

Ammonium Carbonate

2

2

Ammonium Hydroxide

1-2

2

Ammonium Nitrate

2

2-3

Ammonium Persulfate

2

9

Ammonium Sulfate

2

2

Ammonium Sulfide

2

Ammonium Thiocyanide

2

2

Amyl Acetate

4

Amyl Alcohol

3

3-4

Amyl

Chloride

3

3

Aniline

4

Chemical

Ether

Ester

Animal Fats & Oils

2-3

2-3

Antimony Salts

2

•

2

Aqua Regia

4

4

Arsenic Salts

2-1

2

ASTM Oil #1

1-2

1

ASTM Oil #2

2

1

ASTM Oil #3

2

1

ASTM Reference Fuel A

1

1-2

ASTM Reference Fuel B

2

2

Atlantic Oil

1

1-2

Barium Carbonate

2

2

Barium Hydroxide

1

2

Benzaldehyde

3-2

4

Benzene

4

4

Benzene (Gasoline)

(Aromatic)

2-3.

3

Benzoic Acid

2-3

3-4

Boric Acid

1

2

Bromine

2-3

2-3

Bunker Oil

1-2

2

Butane

1

2-3

Butyl Acetate

4

4

Butyl Alcohol

2

3

Calcium Carbonate

2

2

Calcium Chloride

1

2

Calcium Hydroxide

1

2

Calcium Nitrate

2

2

Calcium Sulfate

2

2

Carbon Dioxide

1

1

Carbon Disulfide

2-3

2-3

Carbon Monoxide

1

1

Carbon Tetrachloride

3

4

Castor Oil

1-2

2

Chlorine

2-3

2-3

Chloroacetic Acid

3-4

4

Chloroform

4

4

Chromic Acid

3-4

4

Chromium Potassium Sulfate

2

2

Citric Acid

,

2

2

Cottonseed Oil

_

1

2

Cresol (meta)

4

4

Cupric Chloride

1

2

Cupric Nitrate

2

2

Cupric Sulphate

2

2

Cyclohexanone

4

4

Cyclohexane

2 		2

Chemical

Ether

Ester

Dibutyl Phthalate

3-4

4

Dibutyl Ether

2

2

Dichlorobenzene (Ortho)

3

3

Dodecyl Mercaptan

2-3

2

Diester Oil

2

2

Dimetnyl Acetamide

4 .

4

Dimetnyl Formamide

4

4

DTE Oil (neavy,medium)

2

2-3

Etner

2-3

2-3

Etnyl Acetate

4

4

Etnyl Alcohol (Etnanol)

3

2-3

Ethyl Bromide

3

3-4

Etnyl Chloride

3

3-4

Ethylene Glycol

2

2-3

Esso #90 Lub.Oil

1 .

2

Ferric Chloride

2

2

Ferric Nitrate

2

2

Ferrous Cnloride

2

2

Ferrous Sulfate

2

2

Formaldenyde

3

2

Formic Acid

3-4

4

Freon, 12 or 113

1

2

Fuel Oil

2

2

Gasoline

2

2-3

Glycerine (Glycerol)

1

2

Glycolic Acid

2

2-3

Greases

1-2

2

Heptane

1

2

Hexane

1

2

Hydrazine

4

4

Hydrobromic Acid

2

2

Hydrocarbon Oil

1

2

Hydrochloric Acid, 20%

2

2-3

Hydrofluoric Acid

2-3

3

Hydrogen

1-2

2

Hydrogen Peroxide

,

2

2

Hydrogen Sulfide

3-4

4

,

Hydrolodic Acid

2

2

Iodine Solution

1

2

Isooctane

2

2

Isopropyl Alconol

(Isopropanol)

2-3

3

Isopropyl Ether

2

2-3

CHEMICAL

Ether	Ester

Xylene 								3		3-4

Xylol									3-4		4

Zinc Chloride 							2		2

Zinc sulfate							2		2