Comparison of Adiprene®/Vibrathane®/Duracast® Hot Cast Urethanes to Common Rubbers

Adiprene®/Vibrathane®/Duracast® hot cast polyurethane elastomers are firmly established as preferred or alternate

materials in many industrial applications where various types of rubbers have held sway for a long time. Various types of

polyurethanes, ranging from very hard grades [75 D durometer] to very soft [20 A durometer] and below are commonly used

in a wide variety of applications. “Hardness Ranges” sizes range from giant paper machine rolls and wheels, containing more

than 7,000 pounds [3200Kg.] of polyurethane to very small parts used in office machines, which may contain only a few

grams of material. Some of the reasons for choosing Adiprene®/Vibrathane®/Duracast® hot cast polyurethane elastomers

over the various rubbers are:



















Better abrasion resistance

Better cut and tear resistance

Good physical properties over a wide range of hardnesses

Excellent oil and environmental resistance

Excellent dynamic performance at high load and speed

Ability to fine-tuning of properties for specific applications

Lower set up cost (machines, molds etc)

Liquid castability allows molding by a variety of techniques

Non-marking, non-staining

Most Adiprene®/Vibrathane®/Duracast® hot cast elastomers are processed as two-part liquid systems. Unlike most diene

elastomers (SBR, nitrile, natural rubber, etc.), where the desired elastomer properties are achieved by extensive

compounding of a base stock material, with castable urethanes, compounding ingredients such as fillers, plasticizers and

accelerators are generally not used except in special cases. When a different set of properties is required, the usual course is

to change to a different prepolymer or curative system.

The elastomeric properties of most diene rubbers are due to the cross linking produced in a vulcanization process. This cross

linking allows the flexible segments to extend when the elastomer is stretched, but also provides memory to allow return to

the original dimensions when the force is removed. In castable urethanes, the elastomeric properties are primarily due to the

phase segregation of hard and soft segments in the structure. For this reason polyurethane elastomers are often referred to

as segmented block polymers.

There are many different structures available in Adiprene®/Vibrathane®/Duracast® hot cast elastomers, and each of these

structures provides certain characteristics that can be used to tailor the elastomer to the specific properties needed for the

application. Each polyurethane elastomer consists of a so-called soft segment (based on a polyol) and a hard segment

(consisting of the diisocyanate reacted with a curative). The soft segments can be various polyethers, polyesters and other

polyols, while the hard segments can be various diisocyanates (TDI 1, MDI2 and others) cured with various diamines or diols.

For detailed description of the various structures, please refer to Chemtura Corporation’s Adiprene®/Vibrathane® product

selector guide (can be found on the customer CD or Chemtura Corporation’s website).

.

1

2

1

2

tolylene diisocyanate

4,4’-diphenylmethane diisocyanate

In many applications, polyurethane elastomers compete against various rubbers. Listed earlier are the main advantages of

cast polyurethane elastomers compared to the diene rubbers as a group: These characteristics allow, among other things, for

the parts to stay within desired tolerances for a longer time and extend intervals between replacements. In addition, most

Adiprene®/Vibrathane®/Duracast® hot cast urethanes have natural colors ranging from completely clear to opaque white or

amber. Their ready acceptance of a wide variety of pigments and dyes also permits coloring ranging from black to brilliant

fluorescent oranges, reds and greens. This is especially useful in color-coding of parts. Even when colored black, there is so

little pigment in the polyurethane that the compounds do not leave marks on other surfaces.

Since urethane compounds usually contain no additives that are not tied into the molecular structure (except when plasticized

for hardnesses below about 57 Shore A), there can be no migration of materials out of the elastomer to deposit on other

surfaces. Diene rubbers are subject to ozone cracking, particularly around electrical equipment where ozone concentrations

can be high. Adiprene®/Vibrathane®/Duracast® hot cast urethanes have virtually no ozone-cracking problem. The fact that

urethanes are pourable and castable results in cheaper tooling and fabrication of large parts.

Most rubber compounds when compounded up to 90 or 95 Shore A durometer have sacrificed a good deal of their physical

properties. On the other hand, polyurethane elastomers in the 85 to 95A durometer range are at the peak of their properties

and give extremely good performance at these hardnesses. When possible, urethane parts should be designed to take

advantage of this hardness range. Often, when using urethane for a part that has traditionally been made from a 60-70A

rubber, rather than seeking a urethane of the same hardness it is better to use urethane in the 85-95A range by making the

part thinner, smaller, or by implementing some other design change. This not only results in use of an optimum polyurethane

formulation but results in cost savings to the customer due to reduced material consumption. Table 1 shows some typical

applications for Adiprene®/Vibrathane®/Duracast® hot cast urethanes.

Polyurethane elastomers are available up to about 75 Shore D hardness, and although they begin to resemble hard plastics

in this range, they still have elastomeric properties. There are castable polyurethanes that go as high as 85 Shore D and are

used in a variety of applications, but their properties are more like nylon, polyacetal, epoxy and other plastics and they can no

longer be considered elastomers (Figure 1). On the other hand, polyurethane elastomers that are actually off the low end of

the Durometer A scale are made, and have uses in special applications. Polyether-based Adiprene®/Vibrathane®/Duracast®

hot cast elastomers are particularly resistant to molds, fungi and other microorganisms, making them useful in agricultural,

sewage treatment and tropical applications. While ultraviolet resistance of amine cured polyurethanes in general is good,

darkening usually occurs with outdoor exposure. Therefore, for continuous outdoor exposure, dark colors or pigments are

often used, sometimes in combination with UV-stabilizer packages. Chemtura Corporation also produces special formulations

of Adiprene® prepolymers that are light stable (aliphatic Isocyanates cured with non aromatic curatives are used).

Adiprene®/Vibrathane®/Duracast® hot cast elastomers, particularly the polyester types, are highly resistant to swelling and

deterioration by oils, greases and other non-polar solvents. Finally, the versatility of cast polyurethane elastomers is

unmatched by any other type of rubber. It is often possible to modify one property while holding others more or less

constant. For example, it is possible to formulate higher durometer elastomers with low rebound, lower durometer materials

with high rebound, and vice-versa. Similarly, it is possible to maximize flex life or tear resistance without sacrificing much

compression set over a wide range of hardness. Comparison of the general properties of Adiprene®/Vibrathane®/Duracast®

hot cast polyurethane elastomers with some common rubbers is shown in Table 2. Other important properties, such as

dynamic heat build-up and specific solvent and chemical resistance are not shown, but are available from Chemtura

Corporation. Please contact the technical service team at 1-800-243-2650.

Hardness Ranges – Various Elastomers and Plastics: Figure 1

RUBBERS

CAST POLYURETHANE ELASTOMERS

s

n

o

b

ra

c

o

ro

u

lF

55

65

DUROMETER D

CAST

POLYURETHANE

PLASTICS

20

30

40

50

60

70

80

90

95

DUROMETER A

e

n

e

ly

p

o

rp

y

lo

P

75

85

PLASTICS

e

n

e

ry

ts

y

lo

P

s

n

o

ly

N

s

c

ily

rc

A

s

c

ilo

n

e

h

P

Rubber

Band

45

Auto

Tire

Tread

Mens'

Shoe Heel

50

70

90

100

110

ROCKWELL R

120

130

140

150

Table 2 shows some typical physical properties for various elastomers compared to urethane. Table 3 compares properties

of various Chemtura urethane formulations. For additional information, consult the technical data sheets of

Adiprene®/Vibrathane®/Duracast® hot cast elastomers. These data sheets can be found either on Chemtura Corporation’s

website or on the Adiprene®/Vibrathane® Customer CD.

Typical Urethane Applications: Table 1

Application

Industrial Wheels & Tires

High-Speed Amusement

Park Rides

Power Transmission Belts

Paper Mill Rolls

Office Machine Parts

Oil & Gas Pipeline Pigs

Mining Screens

Polyurethane Type

Adiprene® LF TDI Ester

Duracast® Caprolactone

Adiprene® PPDI Ethers

and Esters

Duracast® Ethers and

Caprolactones

Adiprene TDI® Ethers

Duracast® Ether

Adiprene® LF TDI

Vibrathane® MDI Ester

Vibrathane® TDI Ester

Duracast® Ester

Vibrathane® TDI Ester

Duracast® Ester

Basis of Choice

High load bearing, cut &

tear resistance

Dynamic properties, wear &

abrasion resistance

High load bearing, long

wear life

Hydrolysis, resistance,

hardness stability, dynamic

performance

Long-term environmental

resistance, wear resistance

Abrasion resistance,

petroleum resistance

Long wear, impact

resistance

General Comparison of Polyurethane Elastomers with Various Rubbers: Table 2

Property

Tensile Strength

(MPa)

Durometer

Specific Gravity

Tear Resistance

Abrasion Resistance

Compression Set

Rebound

Gas Permeability

Acid Resistance

Aliphatic

Hydrocarbons

Aromatic

Hydrocarbons

Oil and Gas

Resistance

Oxidation Resistance

Ozone Resistance

Low Temp.

Resistance

Polyurethane

20.7 to 65.5

0A to 85D

1.10 to 1.24

Outstanding

Outstanding

Good

Very high to

Very low

Fair-Good

Fair-Good

Excellent

Fair-Good

Excellent

Outstanding

Outstanding

Excellent

Nitrile

13.8+/

40 to 95A

1.0

Fair

Good

Good

Medium

Fair

Good

Excellent

Good

Excellent

Good

Fair

Good

Neoprene

20.7+/

40 to 95A

1.23

Good

Excellent

Fair-Good

High

Low

Excellent

Good

Fair

Good

Excellent

Excellent

Good

Natural

20.7+/

30 to 90A

0.93

Good

Excellent

Good

Very High

Fair

Fair-Good

Poor

Poor

Poor

Good

Fair

Excellent

SBR

13.8+/

40 to 90A

0.94

Fair

Good-Exc.

Good

Medium

Fair

Fair-Good

Poor

Poor

Poor

Good

Fair

Excellent

Butyl

13.8+/

40 to 75A

0.92

Good

Good

Fair

Very low

Very low

Excellent

Poor

Poor

Poor

Excellent

Excellent

Good

Physical Properties of Typical Polyurethanes: Table 3

Adiprene®/

Vibrathane®

TDI

Polyether

General

Purpose,

Dynamics

Polyurethane

Type

Vibrathane®

TDI

Polyester

General, High

Cut/Tear/

Abrasion

resistance

83A

7100 [48.9]

700 [4.8]

Vibrathane®

MDI Polyether

Adiprene® TDI

Polyether

Duracast®

Polyether

Duracast®

Polyester

Major

Applications

High Resilience,

Hydrolysis

Resistance

High Rigidity,

Wear

Resistance

Dynamics, high

temperature,

hydrolysis

resistance

90A

5600 (39)

100 (7.6)

Dynamics, high

temperature

abrasion

resistance

90A

5700 (39)

1000 (6.9)

Durometer

Hardness

Tensile Strength,

PSI [Mpa]

100% Modulus,

PSI [Mpa]

300% Modulus

90A

4500 [31.0]

1100 [7.6]

85A

5400 [37.2]

820 [5.6]

75D

7500 [51.7]

5500 [37.9]

6599 [44.8]

(@200%)

230

2100 [14.5]

1400 [9.7]

1300 [19.1]

1400 (9.7)

1400 (9.7)

Elongation, %

Tear Strength,

ASTM D-470,

lb/in [kN/m]

Compression

Set, Method B

(22 h@158º

F[70ºC], %

Bashore

Resilience, %

450

600

460

790

650

75 [13.1]

125 [21.9]

80 [14]

145 [25.4]

140 (29.5)

135 (23.7)

27

35

29

1.1 (Method A)

27

47

45

31

64

47

65

55

Manufacturing Methods

Since polyurethane cast elastomers are usually processed as two-part liquid systems, they lend themselves to a wide variety

of molding methods. The working life of the various systems varies from more than an hour to less than a minute, with the

harder grades having the shorter working life. The systems with long working life are usually hand batched (mixed in a

container, and then poured into the molds). Materials with shorter working life must be processed through a high-speed

centrifugal batch mixer or through an automatic meter-mix machine, which prepares, meters and mixes material components

on a continuous basis. With new systems such as Adiprene® Duracast® a variety of processing techniques (hand batching,

tank mixing and machine mixing) can be employed.

Essentially any method for holding a liquid in a certain configuration until it solidifies can be considered a molding method.

Since the molding methods are usually low-pressure and low-temperature. Table 4 lists various methods that can be used

commercially. Some of these will be familiar to the rubber molder. Indeed, in some cases existing rubber molds can be used

to make urethane parts. This is usually a temporary situation however, because lighter and cheaper molds made from a

variety of other materials can be made to replace the heavy, high-pressure rubber molds.

Various Ways to Mold Urethane Prepolymers: Table 4



























Open Casting (most common, easiest, cheapest)

Compression Molding (precision parts)

Transfer Molding (multiple precision parts)

B-Staging (when molds can’t hold hot liquids)

Rotational Molding (makes hollow items)

Centrifugal Molding (pipelining, sheet goods, multi-cavity molds)

Vacuum Casting (wire of fiber inserts in item)

Pressure Casting (pressure chamber to prevent voids)

Liquid Injection Molding (low pressure, bottom fill)

Reaction Injection Molding (high pressure impingement mixing)

Spraying (high pressure solventless & low pressure solvented)

Ribbon Flow® Moldless Casting (for rolls, etc.)

Solvent Casting (low viscosity for fabric penetration)

Open casting is the most common and usually the most economical method since there is little equipment needed other than

an oven or hot table to maintain processing temperature. Additionally there is no pressure applied to the mold. Molds can be

made from many types of materials, including polished steel, aluminum, fiberglass/resin composites, silicone rubber, hard

plastics and castable polyurethane itself. In short, almost any material that can withstand the modest molding temperatures

in the range of 100 to 140 ºC (212 to 284 ºF), which is not porous and does not retain moisture, can be considered as a

potential mold material.

The centrifugal molding technique consists of using centrifugal force to move the material into place and hold it there until

sufficient cure has taken place. It is an excellent method for lining metal, fiberglass or other types of rigid pipe with an

abrasion-resistant polyurethane interior surface. The process consists of introducing the liquid material into the pipe, which

has been prepared with a suitable adhesive, and spinning the pipe at a speed sufficient to distribute the material uniformly on

the walls of the pipe. Spinning is continued until the material is cured enough to stay in place, usually ½ to 1 hour. It is also

widely used to make sheet goods with good dimensional tolerances and surface appearance. In this process, a large heated

drum is used, and the resulting cylinder is slit and placed on a table while still, “green” and allowed to relax into a flat

rectangle.

Vacuum casting is used where air entrapment is a problem. Typical applications are where intricate detail or undercuts in the

mold make air removal difficult. Another important situation is where the casting contains fiber reinforcement or fine wire

windings. The entire mold is placed in a chamber, which is then evacuated. The material is dispensed from the outside

directly from a meter-mix machine or from a supply vessel containing a pre-mixed batch. Degassing is accomplished during

the molding cycle. Pressure casting is used for similar purposes.

Compression molding is a technique borrowed from conventional rubber processing. It is used to make parts to close

tolerances and which must have finished surfaces on all sides. It is also a technique where prototype parts or small

production runs can sometimes be made from polyurethane elastomers using existing rubber molds. The technique consists

of pouring the mixed material into the mold and allowing it to gel to a high viscosity state such that internal pressure is

generated in the mass when the press is closed. With a little experience an operator can learn when to close the press to get

high quality parts every time. Disadvantages of this method are: a), It requires a press with heated platens; b), it does not

lend itself to continuous processing because of the press cycle time, and; c), molds must be of heavy metal construction to

withstand the pressures generated.

For further information on replacing rubber with polyurethane, contact Chemtura’s Adiprene®/Vibrathane® technical service

at 1-800-243-2650.

References:

1)

Adiprene® L 100, Adiprene® LF 1800A and Vibrathane® B 625, Product Bulletins, Chemtura Corporation,

Middlebury, CT.

2)

3)

“Upper Limits: High Temperature Urethanes for Harsh Environments”, M.P. Ferrandino, et al, Chemtura Corp.

“Compounding and Testing for Performance”, Rubber Technology, 1st edition, John S. Dick, Editor, Hanser

Gardner Publications; ISBN: 156990278X, Chapter 9 (2001).

4)

Polyurethanes: Chemistry and Technology, Vol. I and II Interscience, Division of John Wiley and Sons, New

York, NY (1962).

5)

H. Ulrich, Kirk-Othmer: Encyclopedia of Chemical Technology, Volume 23, Third Edition, John Wiley & Sons,

New York, NY, pp. 576-608 (1983).

6)

K.A. Pigott, K.A., “Polyurethanes”, Encyclopedia of Polymer Science and Technology, John Wiley and Sons,

New York, (1989).

7)

8)

C. Hepburn, Polyurethane Elastomers, Elsevier Applied Science, London and New York, (1992).

C. Schollenberger, Rubber Technology, Morton, M. (Ed.) Van Nostrand Reinhold Co., New York (1987).

Appendix

More detailed data is included in this section. Figure 2 lists six specific characteristics that were measured in lab tests,

comparing 6 or more polyurethane systems with several different rubbers. Figure 3 compares compression set values.

Compression set can be helpful in evaluating elastomers in sealing applications. Some PU systems are better than

most rubbers. Figure 4 compares NBS abrasion indices. Polyurethanes are usually better than all rubbers except the

tread rubber. Figure 5 shows that polyurethanes generally have higher tear values and Figure 6 shows polyurethanes

have low heat buildup in dynamic applications. While rubber has slightly higher thermal conductivity, their values are

much different from polyurethane, Figure 7, Figures 8 – 11 show polyurethane’s advantages in fuel and oil

environments. All cast polyurethanes compares quite favorably with a variety of rubbers.

Figure 2

Compression Set by Method B @70C, 20%

Rubber

1) 86A Natural Rubber

2) 62A E-SBR?Cisdene

3)63A NR/CIS BR

4) 52A EPDM

High Modulus PU

1) Duracast S900

2) Duracast C930

Low Modulus Ether

1) PTMEG MDI/ptmeg@95%

2) PPG MDI/bd-tmp-ppg@100%

Low Modulus Ester

1) Ester TDI/MOCA@95%

2) Duracast S700

Low Modulus Ester MDI

1) Ester MDI/ester-bd@99%

2) Ester MDI/bd-ester@98%

80

70

60

50

40

30

20

10

0

Lo Mod Ester MDI

% Set

2

3

hi mod PU

Lo Mod Ester TDI

Lo Mod Ether

4

Rubber

Material Category

Figure 3

91A Caprolactone MDI

1

NBS Abrasion Index- Higher Is Better

Index

2500

Rubber

1)86A NR-Rim Flange Stock

2)62A E-SBR/Cisdene- Tread Stock

3)63A NR/CIS BR- Sidewall Stock

4)52A EPDM- Engine Mount Stock

5)70A Nitrile- wheels and belts

High Modulus PU

1) Duracast S900

2) Duracast C930

Low Modulus Ether PU

1) 62A PTMEG MDI/ptmeg@95%

2) 66A PPG MDI/bd-tmp-ppg@100%

Low Modulus esters (70A systems)

1) Duracast S700

2) 72A Ester TDI/MOCA@100%

Low Modulus Ester MDI

1) 65A Ester MDI/ester-bd@99%

2) 76A Ester MDI/bd-ester@98%

2000

1500

1000

500

0

1

Low Modulus Ether

3

Rubber

5

Material Categories

High Modulus PU

4

Figure 4

Low Modulus Ester (70A

systems)

2

Low Modulus Ester MDI

Tear Strength- ASTM 1938

pli

500

450

400

350

300

250

200

150

100

50

0

1

2

Rubber

1)86A NR-Rim Flange Stock

2)62A E-SBR/Cisdene- Tread Stock

3)63A NR/CIS BR- Sidewall Stock

4)52A EPDM- Engine Mount Stock

5)70A Nitrile- wheels and belts

High Modulus PU

1) Duracast S900

2) Duracast C930

Low Modulus Ether PU

1) 62A PTMEG MDI/ptmeg@95%

2) 66A PPG MDI/bd-tmp-ppg@100%

Low Modulus esters (70A systems)

1) Duracast S700

2) 72A Ester TDI/MOCA@100%

Low Modulus Ester MDI

1) 65A Ester MDI/ester-bd@99%

2) 76A Ester MDI/bd-ester@98%

Rubber

5

Material Categories

High Modulus PU

4

Low Modulus Ether

3

Figure 5

Low Modulus Ester (70A

systems)

Low Modulus Ester MDI

Tangent Delta

0.35

0.3

0.25

0.2

0.15

0.1

1

0.05

3

Low Modulus Ester TDI

Low Modulus Ester MDI

Caprolactone MDI

Rubber

1)86A NR-Rim Flange Stock

2)62A E-SBR/Cisdene- Tread Stock

3)63A NR/CIS BR- Sidewall Stock

4)52A EPDM- Engine Mount Stock

5)70A Nitrile- wheels and belts

High Modulus PU

1)89A PTMEG TDI/MOCA@95%

2)93A Ester TDI/MOCA@100%

Low Modulus Ether PU

1)62A PTMEG MDI/ptmeg@95%

2)66A PPG MDI/bd-tmp-ppg@100%

Low Modulus Ester TDI

1)72A Ester TDI/MOCA@95%

2)72A Ester TDI/MOCA@100%

Low Modulus Ester MDI

1)65A Ester MDI/ester-bd@99%

2)76A Ester MDI/bd-ester@98%

Caprolactone MDI

1)91A Caprolactone MDI/bd

0

5

High Modulus PU

Rubber

Low Modulus Ether

Figure 6

0.4

0.35

0.3

Rubber

1)86A NR-Rim Flange Stock

2)62A E-SBR/Cisdene- Tread Stock

3)63A NR/CIS BR- Sidew all Stock

4)52A EPDM- Engine Mount Stock

5)70A Nitrile- w heels and belts

High Modulus PU

1)89A PTMEG TDI/MOCA@95%

2)93A Ester TDI/MOCA@100%

Low Modulus Ether PU

1)62A PTMEG MDI/ptm eg@95%

2)66A PPG MDI/bd-tm p-ppg@100%

Low Modulus Ester TDI

1)72A Ester TDI/MOCA@95%

2)72A Ester TDI/MOCA@100%

Low Modulus Ester MDI

1)65A Ester MDI/ester-bd@99%

2)76A Ester MDI/bd-ester@98%

0.25

0.2

0.15

0.1

1

0.05

3

2

Thermal Conductivity (W/mK)0

Rubber

High

Modulus

PU

5

Low

Modulus

Ester TDI

Low

Modulus

Ester MDI

4

Low

Modulus

Ether

Figure 7

60

% Shore A Loss after 24

Hours

Rubber

1)86A NR-Rim Flange Stock

2)62A E-SBR/Cisdene- Tread Stock

3)63A NR/CIS BR- Sidew all Stock

4)52A EPDM- Engine Mount Stock

5)70A Nitrile- w heels and belts

High Modulus PU

1)89A PTMEG TDI/MOCA@95%

2)93A Ester TDI/MOCA@100%

Low Modulus Ether PU

1)62A PTMEG MDI/ptmeg@95%

2)66A PPG MDI/bd-tmp-ppg@100%

Low Modulus Ester TDI

1)72A Ester TDI/MOCA@95%

2)72A Ester TDI/MOCA@100%

Low Modulus Ester MDI

1)65A Ester MDI/ester-bd@99%

2)76A Ester MDI/bd-ester@98%

50

40

30

20

10

1

3

0

5

Rubber

High

Modulus PU

Low

Modulus

Ether

Low

Modulus

Ester TDI

Low

Modulus

Ester MDI

Figure 8

% Volume Swell

90

80

70

60

50

40

30

1

3

20

10

0

5

Rubber

High

Modulus

PU

Low

Low

LowModulus

Modulus

ModulusEster MDI

Ester TDI

Ether

Low Modulus Ester TDI

1)72A Ester TDI/MOCA@95%

2)72A Ester TDI/MOCA@100%

Low Modulus Ester MDI

1)65A Ester MDI/ester-bd@99%

2)76A Ester MDI/bd-ester@98%

Low Modulus Ether PU

1)62A PTMEG MDI/ptm eg@95%

2)66A PPG MDI/bd-tm p-ppg@100%

Rubber

1)86A NR-Rim Flange Stock

2)62A E-SBR/Cisdene- Tread Stock

3)63A NR/CIS BR- Sidew all Stock

4)52A EPDM- Engine Mount Stock

5)70A Nitrile- w heels and belts

High Modulus PU

1)89A PTMEG TDI/MOCA@95%

2)93A Ester TDI/MOCA@100%

Figure 9

% Change

Aging 24 Hours in Oil/Fuel

90

80

70

60

50

40

30

1

2

3

4

5

Rubber

High

Modulus

PU

Low

Modulus

Ether

Low

Low

Modulus

Modulus

Ester MDI

Ester TDI

10

0

Low Modulus Ester MDI

1)65A Ester MDI/ester-bd@99%

2)76A Ester MDI/bd-ester@98%

20

Rubber

1)86A NR-Rim Flange Stock

2)62A E-SBR/Cisdene- Tread Stock

3)63A NR/CIS BR- Sidewall Stock

4)52A EPDM- Engine Mount Stock

5)70A Nitrile- wheels and belts

High Modulus PU

1)89A PTMEG TDI/MOCA@95%

2)93A Ester TDI/MOCA@100%

Low Modulus Ether PU

1)62A PTMEG MDI/ptmeg@95%

2)66A PPG MDI/bd-tmp-ppg@100%

Low Modulus Ester TDI

1)72A Ester TDI/MOCA@95%

2)72A Ester TDI/MOCA@100%

Figure 10

Figure 11